## Slide 1: What is Atomistic Modeling?
Prof. Yuan Ping
Department of Materials Science and Engineering
UW-Madison
Last Update: 9/4/24

## Slide 2: What is Atomistic Modeling?
What is atomistic modeling and how do we use it?
Heirarchical or multiscale modeling
The fundamental modeled properties – electronic structure and energy
FCC

## Slide 3: What is Atomistic Modeling?
Using equations that describes how atoms and electrons behave to calculate properties of materials (solids, liquids, gasses, nanoparticles, biomolecules, polymers, etc.)
Structural stability
Electronic structure
Nuclei motion – vibration, rotation, translation
Spectroscopy
Transport
Formation free energy
Band structure, density of states
phonon frequency and modes, dispersion
Electronic and optical excitation,
photoemission, Absorption, Photoluminescence
Carrier mobility, spin diffusion length, mass diffusivity

## Slide 4: What is Atomistic Modeling?
Layer-by-Layer Assembly of Charged Nanoparticles on Porous Substrates: Molecular Dynamics Simulations, J.-M. Carrillo and A. V. Dobrynin, ACS Nano, 5, 3010-3019 (2011)
layer-by-layer assembly of charged nanoparticles adsorbing out of solution onto a porous substrate with cylindrical pores.
Band gap of semiconductors and insulators from QM
M. van Schilfgaarde et al,
Phys. Rev. Lett., 96, 226402 (2006).

## Slide 5: What is Atomistic Modeling?
Examples of atomistic modeling (1 – 1010 atoms)
Stability and structure of nanoparticles
Band gap and light absorption (color) of nanoparticles
Elastic properties of materials under high-pressure
Radiation damage in steels
Qubit states and operation (quantum defects, quantum dots..)
Magnetic properties of Co, oxides, 2D materials
Catalytic reaction mechanisms
Battery cathode intercalation
Some protein folding problems (may join atoms into interacting molecular units)
And so on …
Using equations that describes how atoms and electrons behave to calculate properties of materials (solids, liquids, gasses, nanoparticles, biomolecules, polymers, etc.)
http://www.nec.com/global/corp/H0602.html

## Slide 6: What is Not Atomistic Modeling? Coarse Grained Modeling
Examples >≈ 105 atoms to 10100
Finite element method
Elasticity theory
Fluid dynamics
Car crash simulations
Plate tectonics
Planetary orbits
Using equations that describes how larger scale entities (coarse-grained groups of atoms) behave to calculate properties of materials/systems
http://library.thinkquest.org/25097/graphics/g_main.htm

## Slide 7: Atomistic Modeling Pros and Cons When do we use it?
Pros: Gives complete modeling of every atom virtually on the computer so has the potentials to answer any questions about a group of atoms (which covers almost everything!)
Cons
  Limited accuracy (quantitative (e.g., band/HOMO-LUMO gaps), and qualitative (e.g., wrong ground state for strongly correlated systems))
  Limited time and spatial scales
We use atomistic modeling when the physics can be treated accurately on the length and time scales accessible to atomistic simulation!

## Slide 8: Heirarchical/Multiscale Modeling
If you can directly calculate a property of interest w/atomistic modeling then do it!
If you cannot directly calculate the properties of interest then sometimes you can calculate parameters that can be used in a higher-level model (longer length-time scales) to calculate the property
Example
  What is the rate of mixing (interdiffusion) of two metals at high-temperature when put in contact (cladding/fuel in reactor, Cu wires on Si)
  Direct simulation of mixing is very slow with molecular dynamics
  Can simulate fundamental diffusion constants and then solve diffusion equations

## Slide 9: The Multiscale Modeling Picture Choose your methods based on length/time scales
1nm3 Si ≈ 50 atoms
1cm3 Si ≈ 1022 atoms
http://tu-freiberg.de/fakult4/imfd/cms/Multiscale/multiscale.html

## Slide 10: Essential Atomic Scale Properties
Electronic structure – what are the electrons doing
  Electronic wavefunctions, energies
  Charge density
  Band structure
  Electrical conductivity, optical properties, nature of bonding (ionic vs. covalent), polarization, ionization, valence state, magnetic moments
Energy – how stable are your atoms
  Equilibrium positions, lattice parameters
  Forces on atoms (first derivatives of energy)
  Elastic properties, phonons (second derivatives of energy)
  Phase stability
  Kinetics (depends on forces, energy barriers)
  Thermodynamics (depends on energies)

## Slide 11: A Good Atomistic Modeling Application: Carbon!
http://www.chem.latech.edu/~upali/chem281/image0HQ.JPG
Carbon has many structures – graphite, diamond, nanotubes, buckyballs, diamondoids, …
Electronic structure
  What kind of bonding (sp2, sp3, …)
  Optical properties: band gap
  Conduction: metallic vs. insulating
Energetics
  Stability
  Atom positions
  Thermal conduction: phonon spectra
  Mechanical properties: elastic constants, hardness
http://www.chevrontexaco.com/moleculardiamond/diamondtech/discovery.asp
http://www.nec.com/global/corp/H0602.html

## Slide 12: Summary
Atomistic modeling uses basic laws of physics that apply at atomic scales to calculate properties of interest.
Atomistic modeling differs from coarse-grained approaches (continuum modeling) that do not treat atoms explicitly.
Atomistic modeling yields information about electronic structure and energy, from which many problems can be modeled.

## Slide 13: END