## Slide 1: Quantum Mechanics for Electronic Structure II
Bulk and Periodic Solids
Yuan Ping
University of Wisconsin-Madison
Part of slides from lecture of Shobhana Narasimhan, JNCASR

## Slide 2: Outline
First-principles calculation with periodic boundary condition (crystal)
  Bravais lattice
  Periodic boundary condition
  Bloch theory and reciprocal space
  Brillouin zone
Si crystal
  SCF calculation
  Band structure
  Density of states

## Slide 3: Density Functional Theory
Time-independent Schrödinger equation of multiple nuclei and electrons
Kohn-Sham equations of single electron:

## Slide 4: We can solve a small molecule but…
1023 atoms in 1cm3 solid material
Impossible to calculate directly!
Crystal : solid material arranged in an ordered structure
Utilize this condition to simplify the problem?
…

## Slide 5: Bravais Lattice

## Slide 6: Bravais Lattice
Classified in 7 lattice system and 14 lattices according to symmetry
Centered cell can be further reduced to smaller primitive cell
https://www.physics-in-a-nutshell.com/article/11/close-packed-structures-fcc-and-hcp
https://en.wikipedia.org/wiki/Bravais_lattice
Convention cell (FCC) Primitive cell (FCC)

## Slide 7: Reciprocal lattice

## Slide 8: Reciprocal Lattice

## Slide 9: Born-von Karman boundary condition

## Slide 10: Reciprocal vector
Number of allowed k’s in the 1st (or any other) BZ = Number of unit cells in the crystal, i.e., detd. by size of supercell chosen

## Slide 11: Bloch Theorem
Note that n represents the band index!

## Slide 12: Bloch theorem and DFT
https://www.mathworks.com/matlabcentral/fileexchange/46972-sparse-block-diagonal-concatenation

## Slide 13: K-point sampling
Only a few k-points (101~103) are necessary to get most properties of a bulk!
A few k-points in reciprocal space
Continuous in reciprocal space

## Slide 14: Brillouin zone in reciprocal space
https://en.wikipedia.org/wiki/Brillouin_zone
http://skepticsplay.blogspot.com/2011/10/lot-of-brillouin-zones.html

## Slide 15: Irreducible Brillouin Zone
Smallest wedge of the 1st BZ such that any wave-vector k in the 1st BZ can be obtained from a wave-vector k in the IBZ by performing symmetry operations of the crystal structure.

## Slide 16: Self consistent field (SCF)
ρj
VH, Vxc
ψi, εi
ρj+1=ρj?
External potential
No
Yes
Atomic Density
Finish!

## Slide 17: Self consistent field (SCF) with k-points
ρj
VH, Vxc
ψi, εi (k1)
ρj+1=ρj?
External potential
No
Yes
Atomic Density
Finish!
ψi, εi (k2)
ψi, εi (k2)
Sum

## Slide 18: Plane Wave Expansion of Wavefunction

## Slide 19: Truncating the Plane Wave Expansion

## Slide 21
dg(E)/dE diverges

## Slide 26: Example: Si bulk
FCC lattice
2 atoms in primitive cell
Each Si bonded with 4 Si
Band structures: eigenvalues at each k-points
  Band gap (direct or indirect)
Density of states: number of states at given energy

## Slide 27
Experimental Si Band structure
Calculated Si Band structure

## Slide 28: Practice in terminal
Top left :Applications – System Tools – Terminal
Type commands and press enter to run commands in terminal
Run following commands one by one to start:
  mkdir l2-si
  cp /srv/input_si.zip l2-si
  cd l2-si
  ls
  unzip input_si.zip
  cd input
  xcrysden –pwi scf.in
Opened terminal

## Slide 29: FCC band structure
Special k-points
Xcrysden: Menu-Tools-k-path
https://en.wikipedia.org/wiki/Brillouin_zone

## Slide 30: Tasks
Run a scf calculation to get charge density pw.x < scf.in > scf.out
Run a nscf calculation to get eigenvalues on special k-points pw.x < nscf.in > nscf.out
  Run bands.x and plotband.x to generate data files to plot bands.x < bands.in > bands.out plotband.x < plotband.in > plotband.out
Run a nscf calculation for better density of states plot pw.x < nscf-dos.in > nscf-dos.out
  Run dos.x to generate data files to plot dos.x < dos.in > dos.out
Alternatively, run: chmod +x run.sh after finish: ./run.sh
Plot bandstructure and DOS gnuplot –persist plot.v4.gnu

## Slide 31: Run SCF
‘scf’ for self-consistent-field
set files/folder to read and write and what to write
10.26 Bohr (5Å) FCC cell
2 atoms and 1 types of atoms (Si)
basis set size of wavefunction
Species: Pseudo potentials filename
Position of 2 atoms
6x6x6 K-points
K points 在实空间代表有多少个unit cell

## Slide 32: Run NSCF for band structure
A list of special k-points
5 points along each line
Including more bands to plot
Non-self consistent field: compute eigenvalues and wavefunctions from fixed charge density (no update)

## Slide 33: Run NSCF for density of states
More k-points for better looking DOS and preserve fine DOS structures
(In this example only 6x6x6 for speed)
Specific to make DOS looks better
Non-self consistent field: compute eigenvalues and wavefunctions from fixed charge density (no update)

## Slide 34: Band structure and DOS
Experimental band gap: 1.1eV, indirect
DFT band gap problem: always underestimate gap, 40% to no gap

## Slide 35: Not in class

## Slide 36: Bloch theorem