## Slide 1: Introduction to Many-Body Potentials
Yuan Ping
Credits: Dane Morgan and Giulia Galli

## Slide 2: Outline
Pair vs. many-body potentials
Limitations of pair potentials
Many-Body Potentials
  Bond Order potentials
  Embedded atom potentials
  Charge Transfer terms
  The ReaxFF
  CHARM
  Machine Learning Potentials – IN PROGRESS???
  Coarse-Grained Potentials
Speed and scaling of potentials

## Slide 3: Pair and Many-Body Potentials
Pair Potential: A Hamiltonian for a system of particles that includes only terms of the form f(ri,rj), which include interactions between only two atoms at a time. Generally f(ri,rj) is a central-force, i.e., f(ri,rj) = f(rij=|ri – rj|).
Non-Pair Potential (or Many-Body Potential): A Hamiltonian for a system of particles that includes terms which cannot be written only as functions of two atoms at a time, e.g., f(ri,rj,,rk).
Classical interatomic interactions do not have to involve only pair interactions (even though the basic quantum mechanical interactions are all pairwise!)
Energy
r
Pair interaction f(ri,rj),

## Slide 4: Some Limitations of Pair Potentials Vacancy and Cohesive Energy
(Daw, et al., Mat Sci Reports ’93)
Vacancy-cohesive E relation: Ev (no relaxation)=Ecoh
Any solid (single constituent, 1 atom/unit cell) described with a central pair potential satisfies vacancy-cohesive E relation – but real materials don’t!
Ecoh= E(solid)-E(gas)
Evac
= EN-1(1 vacancy) - EN-1(perfect)
System | Evac/Ecoh
Lennard-Jones, Morse | 1
Ar | 0.95
Kr | 0.66
Ni | 0.31
Cu | 0.37
Pd | 0.36
Ag | 0.39
Pt | 0.26
Au | 0.23
Au: Ecoh = 3.8 eV, Evac = 0.87eV
Kittel, Intro Sol State Phys.

## Slide 5: Some Limitations of Pair Potentials Scaling of Cohesive Energy with Coordination Z
Chart: Coordination Number (Z)
| 1 | 2 | 3 | 4 | 5 | 6 | 7 | 8 | 9 | 10 | 11 | 12
 | 1 | 1 | 1 | 1 | 1 | 1 | 1 | 1 | 1 | 1 | 1 | 1
 | 1 | 0.70711 | 0.57735 | 0.5 | 0.44721 | 0.40825 | 0.37796 | 0.35355 | 0.33333 | 0.31623 | 0.30151 | 0.28868
Pair potential: Bond strength is constant
Real metal: Bond strength decreases ~Z-1/2 (very approximately)
FCC
BCC
(Daw, et al., Mat Sci Reports ’93)

## Slide 6: General Challenges for Potentials
Including essential physics of materials (e.g., electrostatics in ionic materials)
Multibody interactions
Large change in electronic state
  Bond Breaking (e.g., defects, creating surfaces, ...)
  Charge transfer (e.g., Si0+-Si0+ + 2 O0+-O0+ → 2Si4+O24-)
  Directional bonding (e.g., C-C in graphite (sp2 bonding) and diamond (sp3 bonding))
  Magnetic effects (e.g., Fe)
  metal-insulator transition (e.g., high-pressure phases)
  Superconductivity (e.g., MgB2)

## Slide 7: Adding in Multibody Effects Bond Order Potentials (1)
bij includes the many-body effects
bij = z-1/2 “fixes” the coordination dependence problem of simple pair potential
Potentials of this form include Tersoff and Finnis-Sinclair
D.W. Brenner, Phys. Stat. Sol. ‘00

## Slide 8: Adding in Multibody Effects Bond Order Potentials (2)
Z=1, Ecoh = f(r), Ecoh/bond = f(r)
r
r
r
r
Z=2, Ecoh = 3f(r)/2, Ecoh/bond = f(r)/2
bond energy changes with coordination!

## Slide 9: A Multibody Potential For Metals Embedded Atom Method (EAM) (1)
Key new idea: Embedding!
Embedding contribution: each atom is embedded in a host electron gas created by neighboring atoms (Metallic picture)
Have to fit p,G(p), and U(R) to match experimental (or more accurate calculated) data: fit to cohesive energy, vacancy energies, elastic properties, phonon frequencies, etc.
Not equivalent to a pair potential (except when G is a linear function) – can be mapped onto bond-order form (I think?)
(Daw, et al., Mat Sci Reports ’93)

## Slide 10: Adding in Multibody Effects Embedded Atom Method (EAM) (2)
Ecoh = U(r) + 2G(r(r)), Ecoh/bond = U(r) + 2G(r(r))
r
r
r
r
Z=2, Ecoh = 3U(r) + 3G(2r(r)), Ecoh/bond = U(r) + G(2r(r))
If G(2r(r)) ≠ 2G(r(r)) (G is nonlinear) then the bond energy changes with coordination!

## Slide 11: Pt Binding – Many-Body Effects Modified EAM (MEAM) and DFT
DFT shows strong scaling of bond strength with number of neighbors (more neighbors, weaker bonds)
EAM (technicallly the Modified EAM (MEAM), which is EAM with some extra terms) can reproduce this effect
Bulk atom
Surface atom

## Slide 12: A State of the Art Potential ReaxFF (H-C, Si-O, Al-O)
58 Unknown parameters!! Fit to heats of formations, bond lengths, bond angles from quantum calculations and experiment. Quite accurate.
Update – B-C Reaxff has 234 parameters!! Worst I know about. TMS talk, 2017.
W.A. Goddard III, et al., J. Phys. Chem., ’01,’03; Phys. Rev. B ‘04
Esystem = (C-H case)
+ Ebond
+ Eover
+ Eunder
+ Eval
+ Epen
+ Etors
+ Econj
+ EvdWaals
+ ECoulomb
Contains bond-order information – tells the interacting atoms to only see a bond when within a certain range
Correct the bond-order when it over or underestimates the number of bonds expected from valence electrons (e.g., 4 for C, 3 for Al)
Energy associated with deviations of bonds from their ideal bending and twisting angles (e.g., 120º sp2 bonding)
Extra energy associated with pi bond conjugation (from extended networks of pi bonds)
Long-range dispersion forces, short range electron overlap forces
Electrostatic interactions with charges transfer allowed

## Slide 13: CHARM
Widely used potential for (bio-)molecular system. Part of what led to the 2013 chemistry Nobel Prize for Martin Karplus.
Equations are strongly driven by chemical insight with bonding and non-bonding terms, where bonding cover the energies of distorting molecular units.
https://en.wikipedia.org/wiki/CHARMM
https://www.charmmtutorial.org/index.php/The_Energy_Function
https://www.ks.uiuc.edu/Training/Tutorials/science/forcefield-tutorial/forcefield-html/node5.html
Notes: The meanings of right hand side terms are:
First term (summing over bonds): represents the energy between covalently bonded atoms. This harmonic (ideal spring) force is a good approximation near the equilibrium bond length, but becomes increasingly poor as atoms separate.
Second term (summing over angles): represents the energy due to the geometry of electron orbitals involved in covalent bonding.
Third term (summing over torsions): represents the energy for twisting a bond due to bond order (e.g., double bonds) and neighboring bonds or lone pairs of electrons. One bond may have more than one of these terms, such that the total torsional energy is expressed as a Fourier series.
Fourth term (double summation over i and j): represents the non-bonded energy between all atom pairs, which can be decomposed into van der Waals (first term of summation) and electrostatic (second term of summation) energies.
The form of the van der Waals energy is calculated using the equilibrium distance (rij0) and well depth (ϵ). The factor of 2 ensures that the equilibrium distance is rij0. The energy is sometimes reformulated in terms of σ, where rij0=21/6(σ), as used e.g. in the implementation of the softcore potentials.
The CHARMM force field also includes an improper term accounting for out-of-plane bending (which applies to any set of four atoms that are not successively bonded), where kω is the force constant and ω−ω0 is the out-of-plane angle.
The Urey-Bradley term is a cross-term that accounts for 1,3 nonbonded interactions not accounted for by the bond and angle terms; ku is the force constant and u is the distance between the 1,3 atoms.

## Slide 14: Machine Learning Potentials
Recently researchers have been using Machine Learning algorithms to create a potential.
Idea is to consider a large database of energies and forces, call this data Y, and properties of the atomic positions, call this X, and then fit Y(X) not with a physically motivated function but with a machine learned form (e.g., linear regression, Gaussian Process regression, neural networks).
A key complexity is that X should be translationally, rotationally and permutation invariant, which atomic coordinates are not. This can be treated by assuming Yi is the energy of atom i and Xi are a vector of rotationally symmetric functions of the local (<1nm) environment around atom i and fitting Yi(Xi). Then the total energy is E=sum_i Yi. Sometimes one needs to add long-range physics (e.g., electrostatics) in separately.
Generally need more fitting data than traditional potentials (but one can get this from quantum simulations)
See, e.g., Mishin, Acta Mat ‘21

## Slide 15: Coarse Grained Potentials
Remove unnecessary degrees of freedom by grouping together atoms and parameterizing interactions between atom groups
  Speed up calculations
  E.g., CH3 or CH2 might be treated as one object in a protein
Remove unnecessary degrees of freedom by taking out distance dependence on a fixed lattice
  Speed up calculations
  E.g., in the Cluster Expansion potential we use E = E(Cu-Cu)+E(Cu-Au)+E(Au-Au) to describe nearest-neighbor interactions in a Cu-Au alloy on a fixed fcc lattice – no distance dependence makes this simpler!

## Slide 20: Speed and Scaling with Potentials
Each atom interacts with others within a cutoff, typically 5-6 A (a local interaction). This means there is a fixed amount of calculation per atom to get an energy or force if you track the neighbors efficiently. Thus the amount of calculation in a potential scales as O(N) (N=# of atoms). This is called linear scaling. So doubling your system size will typically double the time of the calculation, all other things being equal.
  Quantum calculations generally scale as O(N2lnN) or worse.
  You can also parallelize calculations on many atoms with potentials very well, often up to 100-1000 processors with almost linear scaling. So scaling of time per calculation is more like O(N atoms / N proc)
The amount of work done to get the energies/forces is quite different between potentials, e.g., there is about 1000x as many calculations in ReaxFF than Lennard-Jones, so it is ~1000x slower. Machine learning potentials are similar in speed (~10-100x faster than ReaxFF, 10-100x slower than Lennard-Jones).

## Slide 21: Summary
Many-body potentials include interactions beyond just sums of pairwise interactions. Pair potentials (e.g., Lennard-Jones) cannot explain all the physics in materials.
There are many kinds of many-body potentials which are appropriate for different kinds of physics and vary in speed and difficulty of fitting. Machine learning potentials can model almost any physics but may require a lot of training data.
Potentials are generally about 103-106 times faster than ab initio methods to find energies/forces for a few atoms (millisecond per single energy/force calculation of the system) and scale linearly with number of atoms N (vs. O(N2ln(N) or worse for ab initio methods).

## Slide 22: Adding in Charge Transfer Environment Dependent Electrostatics (1)
E(q) either want to take or give electrons compared to other atoms (e.g., with NaCl, Cl will want to take and Na will want to give)
Optimize whole system to give minimum electrostatic energy while maintaining charge neutrality – this will transfer some charge, but differing amounts depending on positions.
Captures effects of charge transfer on the electrostatics (and can combine with bond-order methods to get many body effects as well).

## Slide 23: Adding in Charge Transfer Environment Dependent Electrostatics (2)
Na solid
No charge transfer
Cl gas
No charge transfer
+
Can lower energy by moving charge from Na to Cl and forming Na+Cl-
Neutral NaCl lattice with no charge transfer

## Slide 24: Charge Optimized Many-Body (COMB) Potentials
Courtesy of Susan Sinnott, Univ. of Florida.
Si nanocluster embedded in an amorphous SiO2 matrix
Si blue (neutral), Si red (charged +), O purple (charged -)
Sinnott Si in SiO2 COMB Charge Equilibration

## Slide 25: Some Limitations of Pair Potentials Perfect Cauchy Relation
Cauchy relation c12=c44  c12/c44=1
Any solid* described with a central pair potential satisfies Cauchy relation – but real materials don’t!
c12=cxxyy
c44=cyzyz
x
y
Stress s
Strain e
y
z
Stress s
Strain e
System | c12/c44
Lennard-Jones, Morse | 1
Ar | 1.1
Kr | 1.0
Ni | 1.2
Cu | 1.6
Pd | 2.5
Ag | 2.0
Pt | 3.3
Au | 3.7
(Daw, et al., Mat Sci Reports ’93)
(Finnis, Interatomic Forces Cond. Matt.)
* I think this is general but perhaps there are some constraints?