## Slide 1: Quantum Mechanics for Electronic Structure II
Bulk and Periodic Solids (Lab)
Yuan Ping
University of Wisconsin-Madison
Part of slides from lecture of Shobhana Narasimhan, JNCASR

## Slide 2: Outline
First-principles calculation with periodic boundary condition (crystal)
  Bravais lattice
  Periodic boundary condition
  Bloch theory and reciprocal space
  Brillouin zone
Si crystal
  SCF calculation
  Band structure
  Density of states

## Slide 3: Density Functional Theory
Time-independent Schrödinger equation of multiple nuclei and electrons
Kohn-Sham equations of single electron:

## Slide 4: Kohn-Sham equation
Ansatz: The ground state density can be represented by a Slater determinant of single-particle wavefunctions
Single-particle wavefunctions (Kohn-Sham orbitals) follows
  : kinetic energy
  : external potential (from nuclei)
  : classical Coulomb interaction between electrons
  : exchange-correlation functional (quantum effect of Coulomb interaction)
Exact to exact solution

## Slide 5: We can solve a small molecule but…
1023 atoms in 1cm3 solid material
Impossible to calculate directly!
Crystal : solid material arranged in an ordered structure
Utilize this condition to simplify the problem?
…

## Slide 6: Bravais Lattice
A system a potential with translation symmetry
: integers
: lattice vector
Subscript for dimensions

## Slide 7: Bravais Lattice
Classified in 7 lattice system and 14 lattices according to symmetry
Centered cell can be further reduced to smaller primitive cell
https://www.physics-in-a-nutshell.com/article/11/close-packed-structures-fcc-and-hcp
https://en.wikipedia.org/wiki/Bravais_lattice
Convention cell (FCC) Primitive cell (FCC)

## Slide 8: Reciprocal lattice
Fourier transform:
For a periodic , is nonzero only at
where
: volume of the unit cell

## Slide 9: Reciprocal Lattice
Every Bravais lattice (in real space) has a corresponding
Reciprocal lattice (in “k-space” or “reciprocal space” ).
The Reciprocal lattice:
Spacing of R’s inversely proportional to spacing of G’s

## Slide 10: Born-von Karman boundary condition
The partial differential equation must be solved with boundary condition
  Molecule : when
The wavefunction must be periodic:
: length of repeat unit
: a (very large) integer

## Slide 11: Reciprocal vector
, ,
For a planewave (eigenfunction of free electrons)
From linear algebra view:
  electron wavefunctions (one per unit cell)
  k-points, each with one wavefunction
  Correspond to same physics and can be transformed each other
Number of allowed k’s in the 1st (or any other) BZ = Number of unit cells in the crystal, i.e., determined by size of supercell chosen

## Slide 12: Bloch Theorem
Note that n represents the band index!

## Slide 13: Bloch theorem and DFT
Single particle wavefunction
  Only wavefunctions with same are coupled with each other!
DFT Kohn-Sham equations :
  For single particle wavefunction
  Block diagonal Hamiltonian
  Can be solved for each individually
https://www.mathworks.com/matlabcentral/fileexchange/46972-sparse-block-diagonal-concatenation
1
2
3
4
5

## Slide 14: K-point sampling
Only a few k-points (101~103) are necessary to get most properties of a bulk!
wavefunctions in real space
k-points in reciprocal space
A few k-points in reciprocal space
Continuous in reciprocal space

## Slide 15: Brillouin zone in reciprocal space
Only one point in is necessary to represent the whole group
First Brillouin zone: The Wigner Seitz cell around the original point
https://en.wikipedia.org/wiki/Brillouin_zone
http://skepticsplay.blogspot.com/2011/10/lot-of-brillouin-zones.html

## Slide 16: Irreducible Brillouin Zone
Smallest wedge of the 1st BZ such that any wave-vector k in the 1st BZ can be obtained from a wave-vector k in the IBZ by performing symmetry operations of the crystal structure.

## Slide 17: Self consistent field (SCF)
ρj
VH, Vxc
ψi, εi
ρj+1=ρj?
External potential
No
Yes
Atomic Density
Finish!

## Slide 18: Self consistent field (SCF) with k-points
ρj
VH, Vxc
ψi, εi (k1)
ρj+1=ρj?
External potential
No
Yes
Atomic Density
Finish!
ψi, εi (k2)
ψi, εi (k2)
Sum

## Slide 19: Plane Wave Expansion of Wavefunction

## Slide 20: Truncating the Plane Wave Expansion

## Slide 22
dg(E)/dE diverges

## Slide 27: Step 1: K-point sampling and convergence

## Slide 28: Born-von Karman boundary condition
The partial differential equation must be solved with boundary condition
  Molecule : when
The wavefunction must be periodic:
: length of repeat unit
: a (very large) integer

## Slide 29: Reciprocal vector
, ,
For a bloch wave (eigenfunction due to periodic potential), where )
Number of allowed k’s in the 1st (or any other) BZ = Number of unit cells in the crystal in real space

## Slide 38: Other practical aspects - poseudopotentials

## Slide 40
Ecutrho = 4 x ecutwfc
for norm-conserving

## Slide 43
si_pbe_v1.uspp.F.UPF
PBE - Vxc
Uspp - poseudopotential
C_ONCV_PBE-1.0.up
PBE – Vxc
Norm-conserving (ONCV) pp

## Slide 49: Example: Si bulk
FCC lattice
2 atoms in primitive cell
Each Si bonded with 4 Si
Band structures: eigenvalues at each k-points
  Band gap (direct or indirect)
Density of states: number of states at given energy

## Slide 50
Experimental Si Band structure
Calculated Si Band structure

## Slide 51: Practice in terminal
Top left :Applications – System Tools – Terminal
Type commands and press enter to run commands in terminal
Run following commands one by one to start:
  CHTC:
  ssh username@spark-login.chtc.wisc.edu
  cd /scratch/username
  cp -r /home/groups/mse_course_ping/examples/QE/silicon/
  cd silicon

## Slide 52: FCC band structure
Special k-points
Xcrysden: Menu-Tools-k-path
https://en.wikipedia.org/wiki/Brillouin_zone

## Slide 53: Tasks
On CHTC, type: sbatch qe-batch-script.sh
On local machine
Run a scf calculation to get charge density pw.x < scf.in > scf.out
Run a nscf calculation to get eigenvalues on special k-points pw.x < nscf.in > nscf.out
  Run bands.x and plotband.x to generate data files to plot bands.x < bands.in > bands.out plotband.x < plotband.in > plotband.out
Run a nscf calculation for better density of states plot pw.x < nscf-dos.in > nscf-dos.out
  Run dos.x to generate data files to plot dos.x < dos.in > dos.out
Alternatively, run: chmod +x run.sh after finish: ./run.sh
CHTC: After finish, download the entire folder to local directory. The visualization software does not work on CHTC.
scp -r username@spark-login.chtc.wisc.edu:/scratch/username/silicon .
Plot bandstructure and DOS gnuplot –persist plot.v4.gnu

## Slide 54: Run SCF
‘scf’ for self-consistent-field
set files/folder to read and write and what to write
10.26 Bohr (5Å) FCC cell
2 atoms and 1 types of atoms (Si)
basis set size of wavefunction
Species: Pseudo potentials filename
Position of 2 atoms
6x6x6 K-points

## Slide 55: Run NSCF for band structure
A list of special k-points
5 points along each line
Including more bands to plot
Non-self consistent field: compute eigenvalues and wavefunctions from fixed charge density (no update)

## Slide 56: Run NSCF for density of states
More k-points for better looking DOS and preserve fine DOS structures
(In this example only 6x6x6 for speed)
Specific to make DOS looks better
Non-self consistent field: compute eigenvalues and wavefunctions from fixed charge density (no update)

## Slide 57: Band structure and DOS
Experimental band gap: 1.1eV, indirect
DFT band gap problem: always underestimate gap, 40% to no gap

## Slide 58: Not in class

## Slide 59: Bloch theorem
All wavefunctions in above conditions can be written as where is a periodic function with period
Proof:
  limited to (first Brillouin zone; see later discussion)
  With periodic potential , is non-zero only for same , solving SE: