## Slide 1: Quantum Mechanics III: Output: bands, forces, stresses, phonons
Yuan Ping
Last Update: 10/8/24
Part of slides from lecture of Shobhana Narasimhan, JNCASR and Dane Morgan, UW-Madison

## Slide 2: Density of States (DOS)
The DOS is a histogram of the number of electronic states per unit energy as a function of energy
DOS are useful for
  Band gaps. Fermi level
  Identifying which atoms/orbitals are contributing to states at what energy
  Simpler to read than band structure – they summarize key information
Projected DOS and projection in general
  Projection of A onto B measures how much of A comes from B.
  One can project sets of wave functions (e.g., from given energy range at the valence band maximum) onto specific atoms, atom types, quantum orbitals (e,g, specific angular momentum) to see contributions to total DOS.
  These projected wave functions can then give projected DOS, Bands, and charge densities.

## Slide 3: Bulk Si Density of States
Gap is about 1 eV (standard DFT get’s this wrong, DFT ~ 0.6 eV, Expt ~ 1.1 eV)
http://en.citizendium.org/images/3/38/Silicon_density_of_states.PNG

## Slide 4: Si Nanoclusters and Effect of Surface Impurities on Band Gap
Band gap from DOS shows changes with surface species
Projected charge densities for HOMO, LUMO states give insight into how the surface species couples to gap (e.g., O localizes the HOMO an LUMO on the oxygen, dramatically changing the gap)
http://what-when-how.com/nanoscience-and-nanotechnology/silicon-nanoclusters-simulations-part-1-nanotechnology/

## Slide 5: Projected Density of States
States are projected on local orbitals with specific angular momentum
Hybridization of the s and p states from both Be and B in the region of 4 eV to 8 eV, implying the tendency to form covalent bonds between Be and B atoms.
Fan, et al, Sci Rep. ‘14
New BeB2 phase

## Slide 6: Band Structure (Periodic Systems)
Solutions for periodic systems have to have the same physics under translations  wave functions are Bloch states: Yn(r+R)=eikR Yn(r), where k is in the first Brillouin zone (this is Bloch’s theorem)
Electronic energy states in periodic systems are conveniently indexed with n,k – n are called the bands, and k the wavevector. The plot of the electronic energy states is called the band structure.
n=1
n=3
n=2
k values (in 1st Brillouin Zone)
Energy of Eigenstates
k*
e1k*
e3k*
e2k*
EFermi
Empty bands
Filled bands

## Slide 7: QM Codes Output: Band Structure CoO2
O(p)
Co(t2g)
Co(eg)
Energy (eV)
Location in Brillouin zone – high symmetry k values are labeled
Fermi level – states at Fermi level  metallic

## Slide 8: QM Codes Output: Band Structure LiCoO2 Band Structure
O(p)
Co(t2g)
Co(eg)
Energy (eV)
Fermi level – no states at Fermi level  insulator

## Slide 9: Relationship Between Band Structure, DOS
https://www.fsis.iis.u-tokyo.ac.jp/theme/nanoscal/periodic_detail/atom_28_Ni/Ni_ggapbe_us_01/Ni_ggapbe_us_01.html
Ni – Can you see the effect of magnetism?

## Slide 10: Forces

## Slide 11: The Born-Oppenheimer Approximation

## Slide 12: Calculation of forces?

## Slide 13: Hellmann-Feynman Theorem

## Slide 14: Hellmann-Feynman Theorem

## Slide 15: Forces in DFT

## Slide 16: Stress

## Slide 17: Computing Forces & Stress with QE

## Slide 18: Forces obtained using QE

## Slide 19: What can one do with forces?
Optimize ionic positions (geometric relaxation).
Force constants, vibrational frequencies.
Molecular dynamics.

## Slide 20: Geometry optimization

## Slide 21: Minimization in 1-D using gradients

## Slide 22: Minimization in an N-d space

## Slide 23: Steepest Descent

## Slide 24: Ionic Relaxation

## Slide 25: Ionic Relaxation
&Control
calculation = ‘relax’
ion_dynamics = ‘bfgs’
QE input:•Tell the program to carry out ionic relaxation, and
say which method to use to find minimum

## Slide 26: Ionic Relaxation in PWscf (contd.)

## Slide 27: The Vibrational Frequency of a Diatomic Molecule

## Slide 28: Frozen phonon calculations

## Slide 29: The Force-Constant Tensor

## Slide 30: Getting Phonon Frequencies

## Slide 31: Forces and Motion