## Slide 1: Molecular Dynamics Length and Time Scales
Yuan Ping
Credits to Dane Morgan’s lectures
Notes: Dane Morgan

## Slide 2: Outline
Temporal scale and rare events
Spatial scale
Accessible process figure
R. Lesar, Introduction to Computational Materials Science, ch. 6

## Slide 3: Limitations of MD – Time Scale (Rare Events), System Size
Time Scale (Rare Events)
  Typically can run MD on only 10-9 s (quantum) or 10-6 (classical) time scale.
  “Rare” events occur very infrequently, so do not happen on MD time scales. These cannot be treated with simple MD.
  E.g., solid diffusion (D ≈ 10-12 cm2/s) has atom hops only every ≈ 10-3 s at room temperature. Cannot see them with normal MD simulations (can use temperature accelerated MD, but that is an advanced topic).
  There are so-called “accelerated MD” techniques to get to larger time scales for some problems, e.g., temperature accelerated, parallel replica, and others. Not totally generally applicable so something of a specialized topic. See reviews from Arthur Voter.
Can we put this all together into a formula for time for a simulation? See next slide

## Slide 4: Limitations of MD – Time Scale (Rare Events), System Size
System Size
  Time for a simulation scales with number of atoms, ie, O(N) for potentials and O(N2lnN) for quantum simulations, and linearly with total time of simulation, ie, O(t).
  Programs can be parallelized to work by spatial decomposition of different regions on different processors.
    For potentials this might allow 106 atoms/core * 103 cores = 109 atoms (106 atoms/core is about maximum as you run out of memory and calculation capacity)
    For quantum simulations this might allow 5-10 atoms/core * 100 cores = 500 atoms (more cores gives poor parallelization for most codes)
  Can typically treat at most 103 (quantum) - 109 (potentials) atoms, and increasing, but still limited.

## Slide 5: Time for A Simulation
Potentials
  Time for 1 energy and force (E/F) calculation= T0 (time for ~1 atoms) x Natoms x 1/Nproc
  Works approximately for Natoms > 1000, Nproc < 1000
  T0 ~ 10-3 s (can vary from 10-4 s to 10-1 s).
  => Big calculation: 109 atoms on 103 processors for fastest potentials takes 102 s per E/F calculation.
  => 104 atoms on 101 proc for typical potential takes 1 s per E/F calculation.
Quantum simulations
  Time for 1 energy and force (E/F) calculation= T0 (time for ~1 atoms) x (Natoms)2ln(Natoms) x 1/Nproc
  Works approximately for Natoms > 10, Nproc < 100
  T0 ~ 101 s (can vary from 100 s to 102 s depending on # of valence electrons).
    Note that technically the quantum scaling is with # of electrons, not atoms, However, Nelectrons is proportional to Natoms for a given fixed stoichiometry. But the elements set the number ration Nelectrons/Natoms and that sets T0.
  => Big calculation: 103 atoms on 102 processors takes 106 s per E/F calculation.
  => 102 atoms on 101 proc takes 104 s per E/F .

## Slide 6: Limitations of MD – Time Scale
Szlufarska and Morgan, private communication
Set by assuming you need 10 hops to get any meaningful statistics and can run for about 10-9 s (quantum) and 10-5 (potentials)

## Slide 7: Summary
Limitations with time (rare events) and system size.
  ~10-9 s (Quantum)-10-6 s (Classical)
  ~103 atoms (Quantum) -109 atoms (Classical)
  No “rare” events
Spatial parallelization is standard, but temporal parallelization is not possible (except in specialized cases, e.g., parallel replica methods).
Within certain ranges of values we can say:
  Potentials: Time for 1 energy and force (E/F) calculation= T0 (time for ~1 atoms) x Natoms x 1/Nproc
  Quantum: Time for 1 energy and force (E/F) calculation= T0 (time for ~1 atoms) x (Natoms)2ln(Natoms) x 1/Nproc