## Slide 1: Molecular Dynamics Analysis: Melting and MD Limitations
Dane Morgan
Last Update: 9/29/21

## Slide 2: Outline
How can I analyze melting in Molecular Dynamics?
Energy vs T
<r^2> vs. T
Method to avoid hysteresis

## Slide 3: Example: Melting Temperature (Tm) From MD
How can I get Tm from an MD simulation?
  What physics determines melting?
  Which ensemble should I use?
  What will I actually calculate that will tell me if the systems has melted?
Simple picture:
Melting is a solid→liquid transition which occurs when we heat the system up enough that the materials stops being an ordered crystal and the atoms start moving around freely.

## Slide 4: Example: Melting Temperature (Tm) From MD
Heating up a solid in a furnace in a lab is the NPT ensemble.
Melting is characterized by
  More motion of atoms: So <r2> for atoms should increase a lot at melting
  Less regular structure: So spatial correlation function should get much more diffuse, maybe with changes in coordination numbers
  New phase with somewhat different density: So we should get a jump in the volume
  Latent heat in the transition: So we should see a jump in the total energy
  Different specific heat in solid and liquid: So we should see a discontinuity in the specific heat

## Slide 5: <Total Energy>=<U> vs. T for LiCl from MD
Amini, et al, J. Phys. C ‘90
CP(solid) = (dU/dt)N,P
Latent heat of transition
Tm
CP(liquid) = (dU/dt)N,P
≠ CP(solid)

## Slide 6: <r2> vs. T for LiCl from MD
Amini, et al, J. Phys. C ‘90
Small displacement in solid – primarily vibrations around lattice sites
Large displacement in liquid – atoms diffuse throughout system
Tm

## Slide 7: Another Approach to Melting Temperature with MD Interface Method
Just heating within NPT ensemble tends to overestimate Tm by 20-30%!! Why? Melting is a first order transition, so the new phase (the liquid) has to nucleate, which tends not to happen on MD time scales until well above Tm.
Another approach: Melting is where the liquid and solid are in equilibrium, so they should be able to coexist. Start with ½ solid and ½ liquid at instantaneous Tinitial≈Tm and let the system equilibrate. Use NPE ensemble. Then temperature will equilibrate to Tm.

## Slide 8: Interface Method to Find Tm
Solid
Liquid
Solid
Liquid
Liquid
Solid
Tinitial>Tm – Solid shrink, latent heat taken in by liquid and kinetic energy decreases T until T≈Tm
Tinitial<Tm – Solid grows, latent heat given off by liquid and kinetic energy increases T until T≈Tm

## Slide 9: Summary
Molecular dynamics can directly simulate a melting process: Melting temperature can be found by jump in energy, trajectories, etc.
Hysteresis effects can be avoided by interface method (also other methods, e.g., thermodynamic integration).