## Slide 1: Example: Si bulk
FCC lattice
2 atoms in primitive cell
Each Si bonded with 4 Si
Band structures: eigenvalues at each k-points
  Band gap (direct or indirect)
Density of states: number of states at given energy

## Slide 2
Experimental Si Band structure
Calculated Si Band structure

## Slide 3: Practice in terminal
Top left :Applications – System Tools – Terminal
Type commands and press enter to run commands in terminal
Run following commands one by one to start:
  CHTC:
  ssh username@spark-login.chtc.wisc.edu
  cd /scratch/username
  cp -r /home/groups/mse_course_ping/examples/QE/silicon/
  cd silicon

## Slide 4: FCC band structure
Special k-points
Xcrysden: Menu-Tools-k-path
https://en.wikipedia.org/wiki/Brillouin_zone

## Slide 5: Tasks
On CHTC, type: sbatch qe-batch-script.sh
On local machine
Run a scf calculation to get charge density pw.x < scf.in > scf.out
Run a nscf calculation to get eigenvalues on special k-points pw.x < nscf.in > nscf.out
  Run bands.x and plotband.x to generate data files to plot bands.x < bands.in > bands.out plotband.x < plotband.in > plotband.out
Run a nscf calculation for better density of states plot pw.x < nscf-dos.in > nscf-dos.out
  Run dos.x to generate data files to plot dos.x < dos.in > dos.out
Alternatively, run: chmod +x run.sh after finish: ./run.sh
CHTC: After finish, download the entire folder to local directory. The visualization software does not work on CHTC.
scp -r username@spark-login.chtc.wisc.edu:/scratch/username/silicon .
Plot bandstructure and DOS gnuplot –persist plot.v4.gnu

## Slide 6: Run SCF
‘scf’ for self-consistent-field
set files/folder to read and write and what to write
10.26 Bohr (5Å) FCC cell
2 atoms and 1 types of atoms (Si)
basis set size of wavefunction
Species: Pseudo potentials filename
Position of 2 atoms
6x6x6 K-points

## Slide 7: Run NSCF for band structure
A list of special k-points
5 points along each line
Including more bands to plot
Non-self consistent field: compute eigenvalues and wavefunctions from fixed charge density (no update)

## Slide 8: Run NSCF for density of states
More k-points for better looking DOS and preserve fine DOS structures
(In this example only 6x6x6 for speed)
Specific to make DOS looks better
Non-self consistent field: compute eigenvalues and wavefunctions from fixed charge density (no update)

## Slide 9: Band structure and DOS
Experimental band gap: 1.1eV, indirect
DFT band gap problem: always underestimate gap, 40% to no gap